| Nominal Votage | 12V |  |
| --- | --- | --- |
| Rated Capacity (10 hour rate) | 200Ah |  |
| Capacity 25℃(77°F) | 10 hour rate (20A) | 200Ah |  |
|  | 3 hour rate (50A) | 150Ah |  |
|  | 1 hour rate (110A) | 110Ah |  |
| Internal Resistance | Full charged Battery 25℃(77°F) | ≤8mΩ |  |
| Cycle Life | 50%(C10) Depth of Discharge | 600 times |  |
| Float Life | 25℃(77°F) Float Voltage 13.8V | Approx. 5 years |  |
| Capacity affected by Temperature (10 hour rate ) | 40℃ (104°F) | 102% |  |
|  | 25℃ (77°F) | 100% |  |
|  | 0℃ (32°F) | 85% |  |
|  | -15℃ (5°F) | 65% |  |
| Self - Discharge 25℃(77°F) | Capacity after 3 month storage | 90% |  |
|  | Capacity after 6 month storage | 80% |  |
|  | Capacity after12 month storage | 62% |  |
| Charging Method 25℃(77°F) | Cycle | Initial Charging Current 50A or small Constant Voltage 14.4-15.0V |  |
|  | Float | Constant Voltage 13.5-13.8V |  |

Packing Dimension

| Product Dimension | mm ±1 | 522×240×242 |
| --- | --- | --- |
|  | Inch | 20.6×9.45×9.53 |
| Package Dimension | mm ±2 | 546×264×290 |
|  | Inch | 21.5×10.4×11.5 |
| Package Number / Carton | 1 |
| Net Weight / Product | 59KG ±200G |
| Net Weight / Carton | 59.0 KG |
| Gross Weight / Carton | 59.5 KG |

Discharge Curves

Physical Dimension

Material

| Component | Positive Plate | Negative Plate | Container | Safety Valve | Terminal | Separator | Electrolyte |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Material | Lead Doxide | Lead | ABS | Rubber | Lead Terminal | Fiberglass | Sulphuric Acid |  |

Discharge Characteristic

| Voltage | Runtime ( Constant Power – Discharge Characteristic 25℃ 77°F ) |  |
| --- | --- | --- |
|  | 3 M | 5 M | 15 M | 30 M | 45 M | 1 H | 2 H | 3 H | 5 H | 8 H | 10 H |  |
| 9.6 V | 8740 | 7600 | 4300 | 2760 | 2060 | 1492 | 840 | 630 | 420 | 280 | 248 |  |
| 10.2V | 8400 | 6500 | 3860 | 2460 | 1980 | 1472 | 810 | 620 | 416 | 276 | 246 |  |
| 10.5V | 7700 | 6160 | 3640 | 2240 | 1940 | 1448 | 780 | 610 | 410 | 272 | 242 |  |
| 10.8V | 7040 | 5860 | 3160 | 2000 | 1880 | 1420 | 760 | 580 | 390 | 270 | 240 |  |